## Slide 1: Towards the production of least contaminant grade biosolids and biochar via mild acid pre-treatment
Presented at the 2023 ANZBP National Biosolids Conference
By
Ibrahim Hakeem
3rd year PhD Candidate (Chemical Engineering)
ibrahim.hakeem36@yahoo.com
Supervisors:
Prof Kalpit Shah A/Prof Jorge Paz-Ferreiro
Dr Aravind Surapaneni
08 February 2023

## Slide 2: Background
https://cbsupplements.com/cc/collagen-peptides-heavy-metals/
A multi-residue analytical method for extraction and analysis of pharmaceuticals and other selected emerging contaminants in sewage sludge - Analytical Methods
Organic matter (40-60 wt%)
Inorganic matter (20-60 wt%)
Inert -Silicates
Ash-forming elements
Heavy metals
PFAS
Microplastics
Heavy metals

## Slide 3: Methodology Design
Biosolids pre-treatment
Pyrolysis
Dry biosolids
Chemical solvents
Leachate
For land application
Treated biosolids
High-grade biochar
Bio-oil: Platform chemicals
Metals Recovery
Biosolids pre-treatment
Solvent type: acids, oxidising agents, chelating agents
Solvent concentration: 1-5% v/v
Solids concentration: 1-20% w/v
Temperature: 25-100 ºC
Stirring speeds: 300-900 rpm
Residence time: 5-180 mins

## Slide 4: Metals removal from biosolids
Table 1: Composition of raw biosolids
Major and trace elements (mg/kg) |  |  |  |  |  |  |  | 
Ca | Mg | Na | K | Al | Fe | Mn | Mo | Ba
44215.3 | 6352.2 | 4747.3 | 6423.8 | 5305.6 | 15133.6 | 273.0 | 5.8 | 229.9
Controlled heavy metals (mg/kg) |  |  |  |  |  |  |  | 
 | Cr | Ni | Pb | Cd | As | Co | Cu | Zn
This study | 21.4 | 35.4 | 23.6 | 1.9 | 3.6 | 3.13 | 1239.8 | 1075.1
C1-grade* | 400 | 60 | 300 | 1 | 20 | - | 100 | 200
C2-grade* | 3000 | 270 | 500 | 10 | 60 | - | 2000 | 2500
Minerals components (wt%) |  |  |  |  |  |  |  | 
CaO | MgO | K2O | Al2O3 | SiO2 | SO3 | P2O5 | Fe2O3 | Na2O
13.2 | 1.0 | 1.2 | 1.7 | 7.1 | 2.9 | 3.3 | 5.7 | 0.3
Chart: Extraction time (min)
| 0 | 30 | 60 | 90 | 120 | 150 | 180
300 rpm | 0 | 0.56218 | 0.53818 | 0.61633 | 0.65362 | 0.68117 | 0.68474
600 rpm | 0 | 0.68012 | 0.65032 | 0.74552 | 0.74818 | 0.79345 | 0.75085
900 rpm | 0 | 0.69493 | 0.68694 | 0.7516 | 0.80676 | 0.76226 | 0.73124
Cd
Chart: Extraction time (min)
| 0 | 10 | 20 | 30 | 60 | 90 | 120 | 150 | 180
1% | 0 | 0.45888 | 0.5656 | 0.54104 | 0.52505 | 0.53305 | 0.54904 | 0.51972 | 0.5677
3% | 0 | 0.35216 | 0.53412 | 0.68012 | 0.65032 | 0.70211 | 0.69478 | 0.73345 | 0.75085
5% | 0 | 0.50157 | 0.60828 | 0.78891 | 0.76759 | 0.8209 | 0.84222 | 0.83862 | 0.78358
Chart: Extraction time (min)
| 0 | 10 | 20 | 30 | 60 | 90 | 120 | 150 | 180
25 | 0 | 0.25142 | 0.34634 | 0.4273 | 0.4528 | 0.44159 | 0.47044 | 0.48766 | 0.47947
63 | 0 | 0.30679 | 0.39718 | 0.52813 | 0.50572 | 0.52187 | 0.58091 | 0.60221 | 0.63782
100 | 0 | 0.35424 | 0.48419 | 0.60082 | 0.644 | 0.67307 | 0.66432 | 0.72076 | 0.75858
Ni
Cu
Fig. 1: Effect of acid type
Fig. 2: Effect of process variables
*according to EPA Victoria biosolids guidelines

## Slide 5
Prospects for critical metals recovery
Metals extraction
Leachate purification pH 4.5
HMs recovery pH 9.0
Treated biosolids
Dry biosolids
3% v/v acid solution
Leachate
Recycled leachate
Conc. leachate
Metal sludge 1
Metal sludge 2
Clarified liquid
NaOH
NaOH/H2O2
Extraction conditions:
Temperature - 25 oC
Time - 30 min
Stirring speeds - 600 rpm
Effects of solids concentration: 1-20% w/v
Leachate purification and HMs recovery:
Case 1: 2-step NaOH co-precipitation
Case 2: H2O2 oxidation pre- NaOH co-precipitation
Case 3: Single step NaOH co-precipitation
Case 4: Biochar sorption

## Slide 6: Results: Metal recovery
Chart: Heavy metals
| Co | Ni | Cu | Zn | As | Pb | Cd | Cr
Two stage NaOH precipitation | 34.4055 | 35.518 | 41.6477 | 97.5896 | 27.1169 | 85.934 | 96.1889 | 96.0411
H2O2 inudced 2-stage NaOH precipitation | 51.4923 | 82.5207 | 61.5146 | 99.4797 | 65.6922 | 85.9362 | 98.1797 | 92.5525
Single stage NaOH precipitation | 32.9007 | 30.6545 | 9.2286 | 99.3189 | 11.3911 | 78.7234 | 98.8532 | 97.4051
Biochar adsorption | 32.129 | 70.5405 | 56.0315 | 56.753 | 18.9617 | 3.7634 | 46.7624 | 47.0858
Elements | As | Cd | Co | Cu | Cr | Fe | Mn | Mo | Ni | Pb | Zn
Raw biosolids | 3.6 | 1.3 | 3.1 | 690 | 20 | 13000 | 210 | 8 | 18 | 20 | 850
5% Treated biosolids | 1.2 | 0.4 | 1.0 | 170 | 14 | 6900 | 10 | 9 | 7 | 18 | 22
10% Treated biosolids | 1.7 | 0.7 | 1.4 | 220 | 14 | 7700 | 17 | 9 | 8 | 18 | 48
C-1 grade | 20 | 1 |  | 100 | 400 |  |  |  | 60 |  | 200
Fig 3: Metal recovery under different methods
Table 2: Metal concentration (mg/kg) in the treated biosolids
H2SO4 consumption of 0.56 g/g dry biosolids
NaOH consumption of 0.50 g/g dry biosolids.
Metal sludge recovery was 0.166 g/g dry biosolids.
Composition (wt%) of metal sludge 1 is 10.7% Fe, 8.8% Na, 8.2% S, 7.9% P, and 5.5% Al
Metal sludge 2 is 13.1% Na, 12.5% S%, 12.4% Ca, 6.0% P, and 3.3% Mg.
C | N | K | P
35.4 | 5.6 | 1.1 | 1.2
32.9 | 5.5 | 0.4 | 0.6
Nutrient wt% in the treated biosolids

## Slide 7
Process flow diagram – Mass balances
Fig 3: Process configuration and mass balances to process 10% solids

## Slide 8
Biochar from pre-treated biosolids
Samples |  | C1-grade* | RBB@500 ℃ | TBB@500 ℃
Biochar yield (wt%) |  |  | 50.7 | 39.6
HMs concentration (mg/kg) |  |  |  | 
As | 20 |  | 5.3 | 3.9
Cd | 1 |  | 2.9 | 1.3
Cr | 400 |  | 40.9 | 28.9
Cu | 100 |  | 2335.2 | 619.6
Ni | 60 |  | 58.3 | 29.4
Pb | 300 |  | 41.8 | 42.3
Zn | 200 |  | 2045.2 | 209.5
Total AAEMs (g/kg) |  |  | 133.2 | 53.67
Ash contents (wt%) |  |  | 52.3 | 41.0
Fixed carbon (wt%) |  |  | 17.6 | 27.7
Volatile matter (wt%) |  |  | 29.3 | 30.7
C (wt%) |  |  | 32.8 | 41.7
H (wt%) |  |  | 1.0 | 1.5
N (wt%) |  |  | 5.5 | 5.6
O/C (polarity) |  |  | 0.18 | 0.13
H/C (aromaticity) |  |  | 0.37 | 0.43
Calorific value (MJ/kg) |  |  | 10.7 | 15.0
Carbon retention (%) |  |  | 44.8 | 51.1
Surface area (m2/g) |  |  | 55.1 | 106.9
RBB
TBB
Table 3: Effects of pre-treatment on biochar properties

## Slide 9: Key Takeaways
Mild sulfuric acid treatment of biosolids can remove 60-85% heavy metals, 70-90% of ash forming elements, and preserve organic nutrients
Cu remain the limiting element to achieve the production of C-1 grade biosolids for unrestricted land application
About 60-95% of dissolved metal can be recovered for potential applications in smelting, inorganic fertiliser, catalysis, and adsorption
Pre-treatment enhanced the production of high quality biochar from biosolids

## Slide 10: Publications

## Slide 11: Acknowledgements
Paul Darvodelsky Scholarship
Supervisory Team led by Prof Kalpit
ARC Transforming Biosolids Training Centre Top-Up Scholarship
School of Engineering, RMIT University Top-Up Scholarship
South East Water Corporation for Resources and Consultation
RMIT University for HDR Scholarship

## Slide 12
Thank you
Let’s get connected
s3822367@student.rmit.edu.au ibrahim.hakeem36@yahoo.com
LinkedIn
Google Scholar